## Slide 1
Robert Zwaska, Fermilab
Muon Collider Accelerator School
6 August 2025
Target Technology

## Slide 2: Fermilab Makes Neutrinos and Muons
Particle accelerators provide the raw material in terms of the kinetic energy stored in the high-power beams
Target Stations convert the kinetic energy into new fundamental particles that are the subject of experiments
  We do this by building devices (targets) that provide reaction material for the matter-creating collisions, focusing devices to maximize the intensities of our beams, and the numerous additional devices and system to manage these beams
This talk: example of making a neutrino beam:
  Interest in neutrinos
  The accelerators provide the raw energy
  The target converts the energy to new matter
  The beamline defines the beam towards detectors
  Neutrinos go forward (inexorably)
A little of the challenges of neutrino beams
Neutrino beams around the world
An introduction to high-power targetry

## Slide 3: The First Neutrino “Beam”
In 1957, Brookhaven AGS and CERN PS first accelerators intense enough to make n beam
  p + Be  p+ + X, p+  m+ n
1962: Lederman, Steinberger, Swartz propose experiment to see
nm + N m- + X (Phys.Rev.Lett. 9, 36 (1962))
n
n
ne + N e- + X
nm + N m- + X
Saw lots of…
Saw none of…

## Slide 4: The NuMI Facility “Neutrinos (ν –> Nu) at the Main Injector”
Intense muon-neutrino beam directed towards Minnesota
Main Injector supplies 25 – 50 trillion 120GeV protons every 1.4 seconds
  Operating regularly above 900 kW
Each pulse produces about 2x1014 ν 
  ~ 20,000,000 Pulses per year
Direct beam 3o down
On-site and off-site experiments
Different types of neutrino beams
Beam is 10s of kilometers wide at exit
Near Detector: 980 tons
Far Detector: 5400 tons
5
Neutrino beam
“Long-baseline”

## Slide 5: Multiple Experiments in the NuMI Beam
Long-baseline oscillation experiments
Neutrino scattering experiments

## Slide 6: Pion Decay!
Most all of our neutrinos come from pion decays
Two quarks, bound together by gluons, convert into a neutrino and muon
A “simple” decay (at first)
  Pion mass ~ 140 MeV/c2, Muon mass ~ 105 MeV/c2

## Slide 7: The NuMI Beam “Neutrinos at the Main Injector”
400 kW design average power
700 kW upgrade for NOvA
1 Megawatt Upgrade 2021
s ~ 1 mm
1 meter long, C target
Produces p+, K+ mesons
Pulsed focusing horns
Toroidal magnetic field
Parabolic inner conductor profile
Focus meson momentum band
2 m diameter
Roughly decay length for 10 GeV p+
He-filled
Absorbs ~ 40 % of beam power
Allows high-energy muons to penetrate
Measure hadron & muon fluxes
Arrays measure distributions

## Slide 8: The MINOS Target
Water cooled
graphite core
Encased in
vacuum / helium can
with beryllium windows
~ 4 kW beam power
deposited in target

## Slide 9: Target Issues
Common failure mode was water cooling
  Also, an issue for horns
  Many lessons were learned in design and in quality control
NOvA target is more robust in its design
  Made possible by being outside of the horn.
  LBNF Design returns to inside the horn
Graphite degradation was observed on one target
  May ultimately limit the performance of the target

## Slide 10: NOvA Target
IHEP Protvino (Russia) initial design
STFC-RAL / FNAL final design and construction
Graphite fins: 50 x 24 mm; 7.4 – 9.0 mm wide
Helium atmosphere
Beryllium windows
Water cooled aluminum pressing plates
Water cooled outer vessel
Initially designed for 700 kW, now upgraded to 1 MW

## Slide 11: Challenging Environments
Replaced NuMI Horn summer 2015 due to failed stripline
  First 700 kW capable horn, in service since Sept. 2013, accumulated ~ 27 million pulses
Failure was due to fatigue, likely enhance by vibrations

## Slide 12: The T2K experiment
Conventional “horn-magnet-focused” n beam
  30GeV Protons on a graphite target
  daughter p+  m++nm (p-  m-+nm )
  Anti-neutrino production by inverse polarity
First application of Off-Axis(OA) beam: 2.0~2.5o wrt. the far detector direction
  Low-energy narrow-band beam
  peak tuned to oscillation maximum
  Small high-energy tail: reduce inelastic bkgs
p
p
n
120m
0m
280m
295 km
on-axis
off-axis
2.0~2.5o
muon-monitor
Near
detectors
Decay volume
Oscillation
Maximum

## Slide 13: Booster Neutrino Beam (BNB)
Uses 8 GeV beam from the Fermilab Booster, operating since 2002
  Up to ~ 30 kW of beam (5e12 ppp)
Beryllium target integrated with single focusing horn
Services a suite of experiments at Fermilab: the Short Baseline Neutrino (SBN) program

## Slide 14: DUNE: Deep Underground Neutrino Experiment LBNF: Long-Baseline Neutrino Facility

## Slide 15: Timeline of High-Power Target Stations at Fermilab
Station | Design Power | Period | Comments
BNB | 30 kW | 2002 – 2027 (?) | 
NuMI | 700 kW – 1 MW | 2004 – 2027 | Megawatt Upgrade in progress.
AP-0 / Muon g-2 | 20 kW | 2017 – 2023 (?) | Using legacy targets & lenses from Antiproton Source.
Mu2e | 8 kW | 2027 (?) - | Very challenging high-Z, radiatively cooled target, even with low power.
LBNF/DUNE | 1.2 MW | 2031 (?) - | Challenging, but achievable devices. Rate of production may be greatest challenge.
Three operating stations, two in various stages of design & construction

## Slide 16: What we don’t want

## Slide 17: Timeline of High-Power Target Stations
Station | Design Power | Period | Comments
BNB | 30 kW | 2002 – 2027 (?) | 
NuMI | 700 kW – 1 MW | 2004 – 2027 | Megawatt Upgrade in progress.
AP-0 / Muon g-2 | 20 kW | 2017 – 2023 (?) | Using legacy targets & lenses from Antiproton Source.
Mu2e | 8 kW | 2027 (?) - | Very challenging high-Z, radiatively cooled target, even with low power.
Mu2e-II | 100 kW | 2030s (?) - | “Impossible” Target
LBNF/DUNE | 1.2 MW | 2031 (?) - | Challenging, but achievable devices. Rate of production may be greatest challenge.
LBNF w/ ACE-MIRT | 2+ MW | 2034 (?) - | Challenging

## Slide 18: PIP-II + Possibilities Numbers are examples, not official
PIP-II itself is a blowtorch of an accelerator
  Capable of 2 mA CW @ 800 MeV -> 1.6 MW
  One could reasonably expect experiments with that beam…
Future accelerators adds even more
  Linac option of 8 GeV?
    16 Megawatt beam
  Linac + RCS
    4 MW @ 2 GeV
    700 kW @ 8 GeV
PIP-II
PIP-III
 | Present | PIP-II | New RCS
MI |  |  | 
Beam Energy[GeV] | 120 | 120 | 120
Cycle Time[s] | 1.33 | 1.2 | 1.45
Protons per pulse[1e12] | 49 | 75 | 190
Power[MW] | 0.7 | 1.2 | 2.5
Proton Source |  |  | 
Injection Energy[GeV] | 0.4 | 0.8 | 0.8-2.0
Extraction Energy[GeV] | 8 | 8 | 8
Protons per Pulse[1e12] | 4.3 | 6.4 | 32
Beam Power to MI [kW] | 38 | 82 | 168

## Slide 19: Timeline of High-Power Target Stations
Stations | Design Power | Period | Comments
BNB | 30 kW | 2002 – 2027 (?) | 
NuMI | 700 kW – 1 MW | 2004 – 2027 | Megawatt Upgrade in progress.
AP-0 / Muon g-2 | 20 kW | 2017 – 2023 (?) | Using legacy targets & lenses from Antiproton Source.
Mu2e | 8 kW | 2027 (?) - | Very challenging high-Z, radiatively cooled target, even with low power.
Mu2e-II | 100 kW | 2030s (?) - | “Impossible” Target
LBNF/DUNE | 1.2 MW | 2031 (?) - | Challenging, but achievable devices. Rate of production may be greatest challenge.
LBNF w/ ACE-MIRT | 2.5 MW | 2034 (?) - | Challenging
800 MeV Exp’t(s) | 1.6 MW | 2030s (?) - | 
2 GeV Exp’t(s) | 4 MW | 2030s (?) - | 
8 GeV Exp’t(s) | 0.8 – 16 MW | 2030s (?) - | 
The Multi-Megawatt
Frontier
Bonus

## Slide 20: High Power/Intensity Targetry Challenges
Target Material Behavior
  Radiation damage
  Thermal “shock” response
  Highly non-linear thermo-mechanical simulation
Targetry Technologies (System Behavior)
  Remote handling
  Target system simulation (optimize for physics & longevity)
  Rapid heat removal
  Radiation protection
  Radiation accelerated corrosion
  Manufacturing technologies
Additional Neutrino Beam Challenges:
Primary beam handling and instrumentation
Accuracy and consistency of all beam inputs, particularly alignment
Focusing elements
Beam-based alignment
Secondary beam instrumentation
Radiation transport modeling
Hadron production
The high statistics from high-power beams require an emphasis on precision

## Slide 21: Nu HPT R&D Materials Exploratory Map
Uncharted Territory
Chart: 
| 6.0200116424043699E+20 | 2.3675941947554702E+21 | 8.02351366000464E+21 | 4.0775233354122002E+21 | 3.9459903245924499E+20 | 1.70992914065673E+21 | 2.6306602163949601E+20 | 3.4198582813134501E+21 | 8.60735916721475E+21
Service | 177059165953070 | 263066021639496 | 526132043278993 | 394599032459245 | 526132043278993 | 368292430295295 | 368292430295295 | 526132043278993 | 389767207571989
Future | 167439867748070 | 334879735496140 | 334879735496140 | 2122065907891940 | 1061032953945970
T2K First Target
LBNF-1.2 MW (CDR)
NuMI-MINOS Target NT-02 (damaged)
NuMI-NOvA Target TA-01 (survived)
LBNF-2.4 MW (Ideal)
Thermal Shock Severity (p/cm2/pulse)
Radiation Damage Severity
(damage equivalent fluence, p/cm2)
LBNF-2.4 MW (CDR)
NT-01
NT-03
NT-07
NT-04
NT-06
NT-05
Future Nu 4 MW
LBNF-2.4 MW Tau Nu
SNS range for 1.4 MW operation for 1 year

## Slide 22: High Power Targetry: Materials R&D
Multi-MW Neutrino Targets & Beam Windows Materials:
Graphite (target core material) studies:
  Swelling/fracture studies
  Preparing for HE proton irradiation at BLIP (2020) to confirm elevated temperature annealing
Beryllium (beam window material) studies:
  Examination of BLIP irradiated Be specimens underway
  Helium implantation studies show bubble formation at irradiation temperatures above 360 ˚C
Titanium Alloys (beam window material) studies:
  Examination of BLIP irradiated specimens underway
  World first high cycle fatigue testing of irradiated titanium underway at FNAL
Benefits to multi-MW targets e.g. LBNF):
alloy/grade choice
cooling system design
tolerable beam intensities
expected lifetimes
RaDIATE
In-beam thermal shock testing of BLIP irradiated Be and Ti alloys at CERN

## Slide 23
Radiation Damage In Accelerator Target Environments
RaDIATE
Collaboration
Broad aims are threefold:
to generate new and useful materials data for application within the accelerator and fission/fusion communities
to recruit and develop new scientific and engineering experts who can cross the boundaries between these communities
to initiate and coordinate a continuing synergy between research in these communities, benefitting both proton accelerator applications in science and industry and carbon-free energy technologies
www-radiate.fnal.gov

## Slide 24
From D. Filges, F. Goldenbaum, in:, Handb. Spallation Res., Wiley-VCH Verlag GmbH & Co. KGaA, 2010, pp. 1–61.
Microstructural response:
creation of transmutation products;
atomic displacements (cascades)
  average number of stable interstitial/vacancy pairs created = DPA (Displacements Per Atom)
Gas production (hydrogen / helium)
Radiation Damage Disorders Microstructure
Slide prepared by V. Kuksenko (Oxford)

## Slide 25
RaDIATE BLIP irradiation summary
181 MeV incoming protons used for RaDIATE irradiation
Irradiation campaign executed in 3 phases with different target box configurations
  6 capsules in target box during each irradiation phase
Total protons on target: 4.57E21 (154 µA avg)
Consisted of 9 capsules from 6 RaDIATE institutions with over 200 material specimens relevant to beam intercepting devices in various current/future accelerator facilities

## Slide 26: BLIP Irradiation Examinations
Significant hardening at low dose in Be and Ti
  Less hardening in higher temperature specimens
First ever fatigue study on irradiated Ti alloys begun
  Indicates about 10% reduction in fatigue strength
Microstructural examinations
Irradiation hardening of S-65F Be
Reduction of strain to failure
Increased strength
Custom Fatigue Testing Machine for Irradiated Materials (FNAL)

## Slide 27: X-ray diffraction – Swelling in BLIP irradiated graphite
W. Bollmann. “Electron-microscopic observations on radiation damage in graphite” Phil. Mag., 5(54):621-624, June 1960.
Simos et al
Impact: Allows confidence to use reactor data for lattice swelling of graphite in HE proton regime for future target facilities

## Slide 28: Neutron irradiated graphite dimensional changes
B.J. Marsden, “Irradiation Damage in Graphite due to fast neutrons in fission and fusion systems,” IAEA-TECDOC-1154, 2000
Big change in c-axis growth ~250 ˚C
Impact: Correlation informs target choice of operating temperature (cooling system design)

## Slide 29: In-Beam Thermal Shock Test: BeGrid2 (HRMT43)
Primary Objectives:
Compare thermal shock response between non-irradiated and previously irradiated material specimens from BNL BLIP (Be, C, Ti, Si)
  First/unique test with activated materials at HiRadMat
Explore novel materials such as metal foams (C, SiC) and electrospun fiber mats (Al2O3, ZrO2) to evaluate their resistance to thermal shock and suitability as target materials
SEM: as-spun Al2O3
Electrospinning concept

## Slide 30: BeGrid2 (HRMT43) – 3-D printed specimen holders

## Slide 31: MIMiC - Methods of Irradiated Material Characterization
        The current routes for high-energy proton irradiations are expensive, long in duration, and lack control of testing conditions and schedule.
        Low-energy ion irradiations are attractive because they allow study of the evolution of the micro-structure during irradiation without activating the specimens, are relatively low cost, and can achieve high dose in very short durations.
        Micro-mechanics and meso-scale testing are potential enabling technologies to overcome some of the limitations of low-energy irradiations as well as to drastically reduce specimen size requirements (which also reduces activity of specimens).
        Ion irradiations and micro-mechanics have been used in the RaDIATE studies on beryllium.
Replicating proton beam interaction damage with minimal residual activity

## Slide 32: Nu HPT R&D Materials Exploratory Map
Uncharted Territory
Chart: 
| 6.0200116424043699E+20 | 2.3675941947554702E+21 | 8.02351366000464E+21 | 4.0775233354122002E+21 | 3.9459903245924499E+20 | 1.70992914065673E+21 | 2.6306602163949601E+20 | 3.4198582813134501E+21 | 8.60735916721475E+21
Service | 177059165953070 | 263066021639496 | 526132043278993 | 394599032459245 | 526132043278993 | 368292430295295 | 368292430295295 | 526132043278993 | 389767207571989
Study | 1782535362629230 | 2.099e+13 | 394599032459245 | 1.1204e+13 | 5000000000000 | 2380957948654750 | 2380957948654750
Future | 167439867748070 | 334879735496140 | 334879735496140 | 2122065907891940 | 1061032953945970
HiRadMat Beam Test - 1
BLIP Irradiation – 2
BLIP Irradiation - 1
Ion Irradiation (planned) MIMiC
Thermal Shock Test (planned) MIMiC
NuMI Be Beam Window
Thermal Shock Severity (p/cm2/pulse)
Radiation Damage Severity
(damage equivalent fluence, p/cm2)
HiRadMat Beam Test - 2
NT-01
NT-03
NT-07
NT-04
NT-06
NT-05
NT-02
TA-01
T2K-1
LBNF-1.2 MW (CDR)
LBNF-2.4 MW (CDR)
LBNF-2.4 MW IDEAL
LBNF-2.4 MW Tau Nu
Future Nu 4 MW
Graphite Fin Studies

## Slide 33: A few notes for Muon Collider Targets
Most comparable configuration is Mu2e – challenging at 8 kW @ 8 GeV.
  Extrapolation to Mu2e-II (100 kW @ 1 GeV) has no present solution
  Cannot Extrapolate to historical Muon Collider (4 MW @ few GeV)
Higher proton beam energy is better for the target (less power deposited in target for the same beam power)
Separating target from optics is very beneficial
  Has the capacity to allow rotation and more robust support systems
  Can more forward production from higher-energy protons be used?
Muon collider requirements on precision may be less strict
Machine Protection is vitally important at high power. Targets and facilities must have this built in from the beginning.
Attempt to avoid liquid targets. Enormous investment and R&D, many risks. SNS, ESS, J-PARC have all decided against liquid targets for new target stations

## Slide 34: Summary
There is broad experience in targets at Fermilab and elsewhere.
Targets are challenging and can be the performance-limiting factor of a facility
There is active development of new targets, and an active R&D program
Muon Collider targets are beyond state-of-the-art; the facility could benefit from choices that allow more buildable targets

## Slide 35
Robert Zwaska, Fermilab
Muon Collider Accelerator School
6 August 2025
Target Technology